OCTG CASING & TUBING* Technical Data

*Oil Country Tubular Goods

MECHANICAL PROPERTIES

Tubing OD: 60.3 to 114.30mm, WT: 4.24 to 16mm

Casing OD: 101.6 to 508mm, WT: 5.21 to 22.22mm

Tubing is used to for extracting petroleum and natural gas from a well. It is the best substitution of EU tubing

we professinal manufacturer of OCTG casing and tubing pipes under the API spec 5CT set in 1996.All the pipes series products can be manufactured as per national or international standards ,including

API5CT,API5L and also ASTM,DIN and  JIS.

| API Grade - 5CT or 5D | Yield Strength - Minimum | Yield Strength - Maximum | Tensile Strength - Minimum | Rockwell C Hardness (est.) |
| --- | --- | --- | --- | --- |
| H-40 | 40,000 psi | 80,000 psi | 60,000 psi | 70-87 HRB |
| J-55 | 55,000 | 80,000 | 75,000 | 0-15 |
| K-55 | 55,000 | 80,000 | 95,000 | 14-25 |
| S-80 | 55,000 | 95,000 | 95,000 | 14-22 |
| C-75 | 75,000 | 90,000 | 95,000 | 14-26 |
| L-80 | 80,000 | 95,000 | 95,000 | 14-23 |
| N-80 | 80,000 | 110,000 | 100,000 | 16-25 |
| S-95 | 95,000 | 110,000 | 110,000 | 22-31 |
| P-110 | 110,000 | 140,000 | 125,000 | 27-35 |
| Q-125 | 125,000 | 150,000 | 135,000 | 30-38 |
| V-150 | 150,000 | 180,000 | 160,000 | 36-43 |
| D | 55,000 | 85,000 | 95,000 | 12-20 |
| E | 75,000 | 105,000 | 100,000 | 16-28 |
| X | 95,000 | 125,000 | 105,000 | 18-30 |
| G | 105,000 | 135,000 | 115,000 | 23-32 |
| S | 135,000 | 165,000 | 145,000 | 32-39 |

DIMENSIONAL & WEIGHT TOLERANCES

| Outside Diameter (OD) | up to 4" | +.031", -.031" |
| --- | --- | --- |
|  | 4 1/2"+ | +1%, -0.5%, not to exceed .125" |
| Wall Thickness |  | +0, -12.5% |
| Weight | single joint | +6.5%, -3.5% |
|  | carload (>40,000#) | +0, -1.75% |
| Drift diameter | up to 2 7/8" OD (42" mandrel) | d-3/32" |
|  | 3 1/2" to 8 5/8" (6" mandrel) | d-1/8" |
|  | 9 5/8" to 13 3/8" (12" mandrel) | d-5/32" |
| Straightness | 4 1/2"+ | 0.2% end-to-end (PE), .125" in 5' at each end |
| Length | Range 1 casing | 16-25' |
|  | Range 2 casing | 25-34' |
|  | Range 3 casing | 34-48' |
|  | Range 1 tubing | 20-24' |
|  | Range 2 tubing | 28-32' |
|  | pup joints (2,4,6,8,10 &12') | +3", -3" |

INSPECTION CLASSIFICATIONS

| Used Tubing/Casing | New Tubing/Casing (and Plain End Drill Pipe) | Used Drill Pipe |
| --- | --- | --- |
| *Yellow Band: 0-15% body wall reduction (85% min. remaining) | *White Band: suitable for all inspections performed (incl. min. 87.5% body wall). | Double White Band (Premium): 80% minimum wall remaining |
| *Blue Band: 16-30% body wall reduction (70% min. remaining) | *Yellow Band: Repairable reject. 87.5% body wall remaining after repair. Locate bands on either side and circle around defect. | Yellow Band: 70% to 80% (min.) of nominal wall remaining. |
| *Green Band: 31-50% body wall reduction (50% min. remaining) | *Blue Band: Imperfections of undetermined depth. Identified as above. | Orange Band: <70% (min.) of nominal wall remaining. |
| *Red Band: 50%+ body wall reduction (<50% remaining) | *Red Band: Defective length. Identified as above. Body wall defects must be cut out of tube. | Red Band: Any tube with a hole or a fatigue crack. |
| Damaged pin or box ends marked with red bands next to pin or on coupling | Damaged pin or box ends marked with red bands next to pin or on coupling | Tool joint classification color bands appear on the pin or box. Shoulder condition color codes are adjacent to the threads. |
| Drift restrictions indicated by green bands on either side of restriction and another next to body wall color band near box | Drift restrictions indicated by red bands on either side of restriction - just like other defects. | N/A |
| *Bands on tube body next to box end or coupling | Tube classification bands appear in same location (box end) as on used material. | Tube classification color bands appear next to the pin |

4.OCTG Grade:

H40, J55/K55, N80, M65, L80/C90, N801/N80Q,  C90/T95, P110/Q125,v150,SY/T6194-96